## Slide 1
Magnetic Random Access Memory
Longlong Zhang
2019.11.25

## Slide 2
Fig 2 A simple model of TMR effect
Part 1 Basic theory of MRAM
Fig 1 A simple model of GMR effect
Fig 0 MRAM model
Note: GMR and TMR are based on the huge resistance difference between parallel and anti parallel states

## Slide 3
Part 2 The Application Of MRAM

## Slide 4
The development of MTJ from 2000 to 2004 |  |  |  |  |  |  |  |  |  |  |  | 
Year | Area(um) | substrate | seed layer | AFM（nm) | PL(nm) | tunnel(nm) | FL(nm) | Cap layer (nm) | Methods | TMR（室温） | 参考文献 | Author
1999 | 2*3 |  | Ta(7) | MnRh(17）/ | NiFe(10)/CoFe(2) | Al2O3(4) | CoFe(4) | Ta(3） | Sputter | 27% | 1999Al-0终结 | 
2000 |  | Si(100) | Pd(15)/Ti(5) | MnIr(16) | CoFe(2.4) | Al-O(1.3) | CoFe(3) | Pd(1.5) | Sputter |  | 2000 MnIr | 
2000 | 6*6 |  |  |  | LaCaMnO3 | NdGaO | LaCaMnO3 |  | PLD | 86%(77K)小 | 2000半金属 | 
2000 | 10*10 | Si(111) | Cr(1.6)Fe(6)/Cu(30) |  | Co(1.8)/Ru(0.8）/CoFe(3) | Al2O3(1.5) | CoFe(1)/Fe(6) | Cu(10)/Cr(5) | MBE | 30%(300k） | 2000人工材料 | 
2001 | 10*10 | GaAs（001） |  |  | Fe(20) | MgO(2) | CoFe(25) |  | Sputter/LA | 27%（300k) | 2001 MgO | Martinez Bou´beta
2001 | 10*10 | SI(001) | Ta(3.5)/NiFe(2) | MnIr(8) | NiFe(4)/Co(2) | Ta2O5(1.8) | Co(2)/NiFe(6) | Ta(3.5) | Sputter | 10%（300k) | 2001TaO | 
2001 | 200*200 | GaAs（001） |  |  | Ga1-xMnxAs(50) | AlAs(1.6) | Ga1-xMnxAs(50) |  | MBE | 70%(8k) | 2001半导体MTJ | 
2002 | 1*2 | STO(001) |  |  | La2/3Sr1/3MnO3(35) | SrTiO3(2.8) | La2/3Sr1/3MnO3(100) | Au(15) | PLD | 1800%（4k) | 2002LaSrMnO | 
2002 | 100*200 | MgO(100) |  |  | Fe(50) | MgO(1) | Fe(5）/Co(50) | Pd(10) | MBE | 17%（300k) | 2002MgO | E. Popova,
2003 | 500*500 | MgO(100) |  |  | Fe(20) | Mg-O(2.6) | FeCo(20) |  | MBE | 23%(4.2K) | 2003MgO | 
2003 | 69*95 | MgO(100) |  |  | Fe(50） | MgO(2.5) | Fe(5)/Co(50) | Au(10) | MBE | 67%(300k) | 2003MgO2 | E. Popova,
2003 | 3*3 | SiO2 | Ru(30) | MnIr(8) | CoFe(2.5) | Y-O(1.5) | CoFe(1)/Py(5） | Ru(10) | Sputter | 25%（300k) | 2003YO | 
2004 | 500*500 | MgO(110) | Au(10) |  | FePt(18) | Al-O（4.5） | CoFe(20) |  | Sputter/EBE | 34%(70K) | 2004FePt | 
2004 | 200*200 | SiO2 | V(42） | /MnIr(10) | Co2MnSi（100) | Al-O（1.8） | CoFe(5.1） | Cu(40)/Ta(5)/Au（40) | Sputter | 33%(300k) | 2004heusler | 
2004 | 3*12 | MgO（001) | MgO |  | Fe(50) | MgO | Fe(10）/Co(10) |  |  | 88%(300K) |  | 
2004 |  | MgO(001) |  |  | Fe | MgO(2.5) | Fe |  | MBE | 180%（300k） | 2004mgo Nature | 
2004 |  | Si（100) | Si3N4/Ru | / CrMnPt | CoFeB | Al2O3 | CoFeB/Ru/FeCo |  | Sputter | 70%（300k) | 2004 CoFeB | 

## Slide 5
The development of MTJ from 2000 to 2005 |  |  |  |  |  |  |  |  |  |  |  | 
Year | Area(um) | substrate | seed layer | AFM（nm) | PL(nm) | tunnel(nm) | FL(nm) | Cap layer (nm) | Methods | TMR（室温） | 参考文献 | Author
2004 | 500*500 | MgO(110) | Au(10) |  | FePt(18) | Al-O（4.5） | CoFe(20) |  | Sputter/EBE | 34%(70K) | 2004FePt | 
2004 | 200*200 | SiO2 | V(42） | /MnIr(10) | Co2MnSi（100) | Al-O（1.8） | CoFe(5.1） | Cu(40)/Ta(5)/Au（40) | Sputter | 33%(300k) | 2004heusler | 
2004 | 3*12 | MgO（001) | MgO |  | Fe(50) | MgO | Fe(10）/Co(10) |  |  | 88%(300K) |  | 
2004 |  | MgO(001) |  |  | Fe | MgO(2.5) | Fe |  | MBE | 180%（300k） | 2004mgo Nature | Shinji Yuasa
2004 |  | Si（100) | Si3N4/Ru | / CrMnPt | CoFeB | Al2O3 | CoFeB/Ru/FeCo |  | Sputter | 70%（300k) | 2004 CoFeB | 
2005 7.8 | 100*200 | Si | Ta(5) /CuN(20)/Ta（3） | PtMn(15) | CoFe(25)/Ru(0.85)/CoFeB(3) | Mg(0.4)/MgO（1） | CoFeB(3) | Ta(5) /CuN（20）/Ta（3） | Sputter | 234% | 2005AA1 | 360/2h/8k0e
2005 | 0.8*0.8 | Si | Ta(5) / Ru(50) / Ta(5) / NiFe(5) | MnIr(10) | CoFe(2) / Ru(0.8) /CoFeB(3) | MgO(1-2) | CoFeB(3) | Ta(5) / Ru(5) | rf Sputter | 260% | 2005AA2 | 375/1h/4koe
2005.10.19 |  |  |  |  |  |  |  |  | Sputter/EBE |  | 2005AA RHEED | 360
2005.8.31 | 1*1 | Si(100) | Ta(10) | PtMn(15) | CoFe(2.5) / Ru(0.85) /CoFeB(3） | MgO(1.8) | CoFeB(3) | Ta(10)/Ru(7) | Sputter | 315%(4k) | 2005AA4 | 360/2h/8k0e
2005.1.24 | 1*1 | Si(100) | Ta(10) | PtMn(15) | CoFe(2.5) / Ru(0.85) /CoFeB(3） | MgO(1.8) | CoFeB(2.5) | Ta(10)/Ru(7) | Sputter | 230% | 2005AA3 | 360/2h/8k0e
2005.10.5 | 3*12 | MgO(100) | MgO(20) | MnIr(10) | Fe(10) | MgO | Fe1−xCox(100) | Au(50) | MBE | 271% | 2005 E-MgO | Shinji Yuasa
2005 | 20*4 | GaAs(001) | GaAs(20) |  | Ga1−xMnxAs(30) | GaAs(1)/AlAs(1.5)/GaAs(1） | CrFe（35） |  | MBE | 14.5（4k) | 2005AlAs | 
2005 | 200*200 | Si/SiO2 |  |  | Pd （1–30）/Co（0.5） | AlOx | Co 0.3/Pd 2 |  | Sputter | 12.60% | 2005 Co-Pd | 
2005 | 10*10 | GaAs | GaAs |  | Ga1- xMnxAs（50） | ZnSe（1） | Ga1-xMnxAs（50) |  | MBE | 100%(2k) | 2005 半导体化合物 | 
4

## Slide 6
Conclusion:
1.The High TMR ratio of MgO-barrier MTJ based a solid foundation for the future development of MRAM device.
2.After the year of 2007 ,most of groups are satisfied with the TMR ratio of MRAM and changed their research direction to improve other aspects of MRAM performance.

## Slide 7
The development of MTJ from 2007 to 2019
Apart from the TMR ratio , device area ,switching time , and write error rate are also vital aspects of MRAM.
TMR Ratio
device area
1998
2007
TMR Ratio
Switching time
STT
SOT
VCMA
…
Out of plane magnetization MRAM
Dual interface MRAM
PSA –MRAM
Magnetoelectric coupling

## Slide 8
LLG Equation

## Slide 9
LLG Equation(2)
Transformation of the two expression

## Slide 10
LLGS Equation

## Slide 11
STT Simulation

## Slide 12
STT Simulation(2)

## Slide 13
spin polarization vectors
Nanotechnology 30 (2019) 375202
STT
SOT
SOT Effect

## Slide 14
Model 2 Anisotropy(1, 0, 100) Fixed later (-1, 0 ,0)
SOT simulation

## Slide 15
SOC Coupling
In quantum physics, the spin–orbit interaction (also called spin–orbit effect or spin–orbit coupling) is a relativistic interaction of a particle's spin with its motion inside a potential.
magnetic moment of the electron
The energy of a magnetic momen
Magnetic field

## Slide 16
NATURE NANOTECHNOLOGY | VOL 4 | MARCH 2009
Figure 1 | Schematic of the sample used for a voltage-induced magnetic anisotropy change
Voltage Control Magnetic Anisotropy

## Slide 17
2011 The Japan Society of Applied Physics
Voltage Control Magnetic Anisotropy（2）

## Slide 18
E
V）
Voltage Control Magnetic Anisotropy（3）

## Slide 19
ABSTRACT:A giant, reversible and nonvolatile electric-field manipulation of magnetoresistance to
about 55% is realized at room temperature without the assistance of a magnetic field.
Magnetoelectric coupling

## Slide 20
Note: There is a energy barrier between the P state and the AP state ,to ensure high stability of MRAM we should let . But,with the decrease of the sample area the energy barrier drop too.
A: cross sectional area of the device
interface anisotropy
MTJ
P-MTJ
PSA-MTJ
Huge Demage
Device Area

## Slide 21
Device Area (2)

## Slide 22
MTJ
P-MTJ
Dual interface MTJ
PSA-MTJ
Dual interface PSA MTJ
Time Direction
Device Area(3)